## Slide 1
Introduction of Welding Applications November 2023
Presented By

## Slide 2
Battery Weld Application- Cu Tab
Why use Copper-alloy tab?
Battery Performance Improvement
High electric and thermal conductivity suppresses temperature rise
-Reduce high-current charging/discharging time
-Increase battery cell life
Cost Reduction
Material cost is lower than nickel
No projection or slitting process is required, reducing the manufacturing process
Cylindrical battery
Sn plating
Copper-alloy tab
Battery

## Slide 3
Battery Weld Application- Cu Tab (continued)
Nickel and copper-alloy bonding form differences
Welding example (peeled joining area)
Nickel
Nugget is formed at the bonding interface
Joining area between Ni tab and battery case
Cu Alloy (Sn Plating)
Nugget is NOT formed at the bonding interface
Joining area between Cu alloy tab and battery case
Welding example (cylinder side)
Welding Mark
(No melting)

## Slide 4
Battery Welding Application- Avio Improvement
Avio Resistance Welder Benefit
Enable high quality welding of copper alloy tabs, which is difficult for previous welding controllers
High-Reliability Inverter Type Resistance Welder
Avio NRW-IN400PA/NT-IN8444B
Fast ramp-up for quick heat generation
High peak current hold for longer welding time allowing diffusion bonding
Control Frequency: 5 kHz
Maximum Weld Current: 8,000A
Ideal for Battery Tab Welding!
Image of current waveform
Time
Current
High peak Current holding
High welding cycle
Avio
High
Fast
ramp-up
Time
Current
Competitor
(Transistor-type)

## Slide 5
Wire Fusing Weld Application
High-Reliability Inverter Type Resistance Welder
Avio NRW-IN900P/NT-IN32K444B
Motor
Multiple insulated wires
Terminal
Control Frequency:5kHz
Maximum Weld Current: 32,000A
Ideal for Wire Fusing!
Why is wire fusing better than soldering?
Direct joining without solder has higher connection reliability
  Heat resistance improvement
  Vibration resistance improvement
High productivity
  No insulation stripping required
  Shorter process time

## Slide 6
Wire Fusing Welding Application
What is Wire Fusing?
Deformation by heat and pressure allows the insulation to be removed while ensuring electrical conduction and strength of the bond… “Fusing” method
Precise control of the crush finish dimensions are required to ensure the quality of joining
Pressure
Terminal
Electrode
First
Current
Electrode
Second Current
Covered Wire
The insulation is removed and current flows through the wire to heat and bond
Current flows only in the terminal
Heating terminal
Complete the joining

## Slide 7
Wire Fusing Welding Application- Avio Improvement
Avio Resistance Welder Wire Fuse Benefit
[Pulsation Mode]: Precisely control the heat input with fine, “pulse like” current control
Gradual heating prevents excessive crushing
Pulsation Mode
Conventional
External signal
Current
Adjust current output based on predetermined PLD settings
Reduce current output to
maintain proper crush
Sensor Input Compensation
Added control using input of external pulse signals including displacement sensors and current output level correction during the weld process
Fine tune crush level and better control insufficient or excessive crush

## Slide 8
Harness Welding Application
Ideal for Harness Welding!
Harness
Copper Harness
Aluminum Harness
High Power Ultrasonic Metal Welder
SE-10K (Provisional Name)
Scheduled to be released in 2024!
Control Frequency:20kHz
Maximum Output Power: 10kW
New Product
Why is direct bonding better than crimping?
High connection reliability
Low contact resistance suppresses heat generation
  Improvement of bonding strength, heat resistance and vibration resistance
Capable of joining dissimilar metals
  Join aluminum harnesses and copper terminals
  Weight reduction from utilization of lighter materials

## Slide 9
Harness Welding Application- Avio Improvement
High voltage harness
EV aluminum harness
EV bus bar
High-capacity laminated battery (laminated foil and tab)
Applicable assemblies:
[Run chart monitor]
Visualization of process transitions
Judgment of joint results
Monitor for proper replacement of joining tools
Monitor for predictive failure
Process time reduction using 10kW high power
Larger diameter stranded wire, such as 100SQ class, can be joined in just a few seconds
Extensive monitoring functions improves quality control
Better equipment maintainability and control
Ultrasonic metal welder benefit

## Slide 10
www.avio.co.jp
www.easleyllc.com
Thank you